PRODUCT:	 			         6OPU979Gx0

DESCRIPTION:			         Clear Acrylic Self-Sealing Exterior Topcoat

USE:					         Exterior Kitchen Cabinetry and Furniture

APPLICATION SYSTEM:	         Traditional Spray guns, Airless, Airmix

# CHEMICAL - PHYSICAL CHARACTERISTICS*

SPECIFIC GRAVITY: 			1.010 + 0.100 (Kg/l at 68°)

DENSITY (WPG):  			8.43 + 0.100 (lbs/gal US at 68° F)

WEIGHT SOLIDS: 			46% + 1

VOLUME SOLIDS: 			78.93% + 1

VISCOSITY:					100"+ 2” (DIN6 at 68° F) approximately 80” Zahn cup n°4

VOC (material):                                    4.55 lbs/gal US or 545.40 g/l

VOC (coating):                                     4.55 lbs/ga US or 545.40 g/l

VOC Ratio:                                           1.17 lbs VOC/lbs Solids

HAPS Ratio:                                         0.49 lbs HAPS/lbs solids

*All values based on 20 sheen

PREPARATION OF THE PRODUCT

6OPU979Gx0				100 parts by weight

6CTN52					  20 parts by weight

DPU820 / SOL-9054	                      30-40 parts by weight

Or

6OPU979Gx0				100 parts by volume

6CTN52					  20 parts by volume

DPU820 /SOL-9054		            35-45 parts by volume

POT-LIFE:		                               3 hours

This product meets U.S.A. TSCA regulations.

APPLICATION CHARACTERISTICS

APPLICATION AMOUNTS:                100-110 g/mq  2 - 4 (wet mils)

NUMBER OF COATS:			1 – 2 coats

DRY TIME:

At 68° F (4 wet mils)

- DUST FREE:		          		30-35 Minutes

- MARK-PROOF:		          		60-70 Minutes

- DRY TO SAND:				       2 Hours

- STACKABLE: 		          		     24 Hours

Available in 10, 20, 30 and 80 sheens.

GENERAL PROPERTIES

This product is a Clear Self-Sealing Acrylic Exterior Topcoat made for exterior projects in need of extreme weathering resistance. It offers excellent resistance towards external exposure and UV rays.  It is best to dilute the first coat to allow the coating to dive into the substrate. It is also suggested to use this product with tinted impregnators. This product is not designed to be applied on deck flooring or other walkable surfaces.

For further information, please refer to our technical representatives.

SHELF LIFE: 3 Years

Data refers to product stored in original, sealed packing.

STORAGE:  Keep in a cool, well ventilated place; temperature should not exceed 77°- 82.4° F.

Company Information: SIRCA S.p.A. has a quality system certified by DNV GL ISO 9001



The information supplied are correct to the best of our knowledge. However, as the coating process depends on many variables and the present application takes place without our supervision, we cannot assume any responsibility for the final result. Sirca guarantees that chemical and physical characteristics of the products are within the reported range. Due to the large variety of substrates and

application devices, the purchaser/user should test our products in his own application conditions and safety and environment circumstances. Sirca’s technical and sales departments are at customer’s disposal for any further information regarding correct application of our products.

# Text boxes

6OPU979Gx0

12 - 2022

TECHNICAL

DATA SHEET